## Slide 1: Additives
Wan Sharuzi Wan Harun
Faculty of Mechanical Engineering Universiti Malaysia Pahang
sharuzi@ump.edu.my
jihad_ku@yahoo.com
019 959 0039
09 424 6339
Plastic Injection Technology BMM 4843

## Slide 2: INTRODUCTION
In addition to the raw plastic materials, there are a number of other ingredients that may be added to the plastic to modify its properties.
These other ingredients are referred to as additives and include plasticizers, fillers, reinforcements, stabilizers, flame retardants, colorants, lubricants and many others.
It is essential that the engineer understand the need for some of the additives and their impact on the molding process.

## Slide 3: 1. Fillers & Reinforcements
Fillers and reinforcements are added to the plastic primarily to increase the stiffness of the plastic part and/or increase the other mechanical properties of the part.
Additives that are used to increase the mechanical strength of the part are usually referred to as reinforcements.
Common fillers include calcium carbonate (powdered limestone), talc (powdered mineral that has a slippery or soapy feel), carbon black (as a black colorant and, as a protector against UV radiation) and silica (a very small, spherical-shaped mineral).

## Slide 4
Most of the reinforcements added to plastics take the form of small fibers, powders or flakes.
The most common reinforcement is a glass fiber that is like a very fine monofilament [.009 to .013mm in diameter].
The strands are cut to short lengths (less than 6.35mm) and added to the plastic when it is formulated.
Glass fiber reinforced nylon and polyester materials are quite common and are quite strong, often replacing die cast metal parts.

## Slide 5
The glass reinforced material requires special molding considerations and is very abrasive to the metal surfaces with which they come into contact.
As if these are not enough, fibers are also made from carbon, graphite, and metal, enhancing the resulting part strength and even further complicating the molding of the parts.
Some metal fiber reinforcements are added to provide electrical conductivity.

## Slide 6
In addition to powder and fiber forms, some reinforcements are in the form of a flake.
These flake reinforcements include those made from mica (a lightweight mineral), glass and aluminum.

## Slide 7: 2. Plasticizers
Plasticizers are used to reduce the stiffness of the plastic part, making it more flexible.
In achieving the increased flexibility, plasticizers may also reduce the viscosity of the melt and function as a lubricant.
Plasticizers are frequently used in producing parts made from PVC, increasing part flexibility to a "rubbery" feel.

## Slide 8: 3. Stabilizers
PVC is a common object of both heat stabilizers and UV stabilizers.
When PVC is processed at too high temp, degradation will occur and may be associated with the release of hydrochloric acid.
Heat stabilizer are mixed with the plastic to help prevent degradation from excessive heat in processing.
Also important that the stabilizers be compatible with the resins to which they are added to avoid chemical or viscosity problems in molding.

## Slide 9
UV stabilizers are also important because they increase the molecular stability of plastics that are exposed to light.
UV stabilizers help increase the ''weatherability" of plastics exposed to sunlight in outdoor environments.

## Slide 10
Each of everyday lives plastic product and equipment that people use, the degree to which each is flammable is very important.
Plastic products of the home, automobile, boats, and airplanes must be as resistant to burning and smoke generation as possible.
As a result, flame retardants and smoke suppressants are added to many plastics to control the undesirable effects that can result from combustion.
4. Flame Retardants

## Slide 11
Flame retardants are added directly to the material when formulated allowing the molder to purchase flame retardant grades of material.
Unfortunately, most of these additives are corrosive to the metal surfaces to which they are exposed, requiring special protective coatings to be used in the injection unit and the mold.
They also may accelerate resin degradation and restrict the heat profile.

## Slide 12
One of the advantages of manufacturing parts from plastics is avoiding the need to paint the molded product.
Colorants may be added to the plastic allowing the entire part to be colored, not just the surface.
In order to accomplish this, pigments and dyes are added to the plastic, either as a part of the formulated plastic pellet, an additive pellet of colorant or as a liquid that is added to the plastic after it enters the injection unit.
5. Colorants

## Slide 13
Pigments are not soluble in the plastic melt but are mixed in by a dispersion process.
Dyes are soluble and provide maximum color strength and brilliant at minimum cost.

## Slide 14: Case Study 1
One molder found that the change from processing a non-reinforced material to one reinforced with fiberglass fibers required that his screws needed to be manufactured from a more wear resistant material, have deeper flights and less compression.
In addition, he learned that the heat profile needed to be greatly altered to achieve the proper quality melt.

## Slide 15: Case Study 2
Another molder discovered that the addition of carbon black to the HDPE he was processing required a screw that more aggressively mixed and sheared the material or the resulting melt had ''windows" or unmixed areas that would adversely affect the ''weatherability" of the resulting product.

## Slide 16: Today’s Quiz
A molder was adding titanium dioxide to his material to alter the color of his parts. The Ti02 is a commonly used additive to achieve a very white coloration of the parts produced.
However, in a very short time, the molder discovered severe wear in his barrel and screw.

## Slide 17
Research revealed that, the Ti02 can be very abrasive.
As an expert in injection molding process, you are tasked to solve the stated problem.
  Determine the potential section on the IM machine that requires attention to solve the problem.
  Suggest the action needed to overcome the problem.

## Slide 18: Answer to Quiz
It is requires that the injection unit components (screw, barrel, valve and end cap), and sometimes the runners and gates in the mold, be made from more wear resistant materials.
In this case, the components were replaced with different, wear resistant materials and the wear previously experienced was no longer a problem.

## Slide 19: Today’s Quiz Again
A FKM molder was using silicone as an additive in his process.
Silicone is known for its chemical and physiological inertness and has good physical and electrical properties that don't change significantly from very low to very high temp.
Silicone is also water-repellant and anti-adhesive and is used as a lubricating agent, an anti-foaming agent and foam stabilizer.

## Slide 20
However, after processing for a time, the molder began to observe tiny metallic particles embedded in the parts.
  Identify potential sources of the identified tiny particles that found on the molded parts.
  Discuss action required to be taken to eliminate the problem.

## Slide 21: Answer to Quiz
The silicone erodes certain flight hard-surfacing materials used on the flights of screws.
The screws were rebuilt and chrome-plated completely over the entire surface of the flights.

## Slide 22: The lesson learnt
Any time an additive is added to a material, there will be an important effect on the molding process that will likely require changes in the processing profile and/or equipment.
Be alert for these effects and take corrective action before costly remedies are needed!