## Slide 1: Control
Wan Sharuzi Wan Harun
Faculty of Mechanical Engineering Universiti Malaysia Pahang
sharuzi@ump.edu.my
jihad_ku@yahoo.com
019 959 0039
09 424 6339
Plastic Injection Technology BMM 4843

## Slide 2: INTRODUCTION
A control system on the IMM is required to cause the clamp unit, the mold, and the injection unit function properly with any degree of automation.
Essential elements of the control system are;
  Controlling
  Monitoring

## Slide 3: Processing Functions
Clamp Unit Control
  Control over the speed of moveable platen (and the mold) opens and closes without jerking.
  How far the platen opens and the amount of clamp tonnage pressure exerted to hold closed the mold.
  Controls some vital safety setting that prevent the mold from closing under abnormal conditions.

## Slide 4: Processing Functions
2. Extruder (Screw) Control
  The speed of the screw rotation (RPM or % of maximum speed) and the amount of back pressure are determined with this control.
3. Temperature Control
  Controls the temp. settings of the heater bands on the barrel and the nozzle.
  Each heater band zone and the nozzle may independent set at the specific temp. desired.

## Slide 5: Processing Functions
4. Injection Control
  Control of the shot size.
  The fill speed or velocity of the screw as it comes forward during injection.
  The transfer point where the screw speed reduces to commence the holding of the screw in place until the sprue freezes off.
  The hold pressure setting that are required while the part(s) are cooled and solidify.

## Slide 6: Processing Functions
5. Core Pull
  The selection of the core pull sequence and the positions required are determined by this function.
6. Ejector Control
  The speed, position, and forward limits of ejection are determined in this function.
  Multiple or pulsing ejection is also controlled as is retraction speed and limits of ejectors performing multiple ejection.

## Slide 7: Processing Functions
7. Purge Control
  Control over the purging of the barrel of unwanted plastic, whether to shut down, change color or other purposes.
  The screw rotate speed, back pressure limitation, purge time and number of purge cycles that are normally controlled manually, may be controlled automatically.

## Slide 8: Control Functions
1. Manual mode
  Where the limits may be set to desired parameters, but the machine will not perform any functions unless an activate button engaged.
  This mode is typically used in starting up a mold or shutting down and purging.
2. Semi-Automatic mode
  All the machine limits are preset but the machine stops at the end of the cycle.
  Will not commence a new cycle until the machine safety gate is opened and closed.
  Commonly used where ejection must be done manually or with manual assist (by the operator) or when a mold is just starting up.

## Slide 9: Control Functions
3. Automatic mode
  All machine limits are preset and the machine cycles repeatedly unless stopped by a safety condition or by the operator.

## Slide 10
Indicating that the core sections, cavity sections, and the runner system is contained within two plates or three plates in the mold.
The runner system includes the sprue (main channel through which the molten plastic enters the mold) and the runners (smaller channels that carry the plastic from the sprue to the cavities and cores).
As the molten plastic between the cores and cavities cool and solidify, so does the plastic in the sprue and runners.

## Slide 11
Figure 7.1 Two plate mold in a closed position

## Slide 12
As shown in figure 7.1, its referred to as a two plate mold because the parts and the runner system are all contained within two plates, The A plate and B plate.
Two plate mold is the most common types of mold in use.
Besides the two plates referred to as the A and B plates, there are three other plated that comprise the main element of the mold. All of these plates, are referred to as the mold base.

## Slide 13
The gate is a small opening where the molten plastic moves from the runner system into the part.
Figure 7.2 Two plate mold in an open.

## Slide 15
When the mold opens, where the movable platen retracts, the parts and runner system stay on the core half of the mold. The sprue puller pulls the sprue out of the sprue bushing.
Figure 7.3 Two plate mold shown at ejection

## Slide 16
The runner systems needed to serve a mold that is making a number of parts in one shot.
Two common designs of runner.
  Circular
  Symmetrical
All designs must be balanced, that is the distance from the sprue to each part has the same length and flow volume.

## Slide 17
Figure 7.4 Illustration of two balanced runner systems

## Slide 18: Runner & Gate

## Slide 19: Runner Cross Section
Three conventional runner profiles
Parting line
Sometime calls

## Slide 20: Runner Cross Section
All runner cross sections are focuses on minimize liquid resistance and temperature reduction when molten polymer flows into the cavity.
  Too big
    Longer cooling time, more material, costly
  Too small
    Short shot, sink mark, bad quality
  Too long
    Pressure drop, cooling, waste

## Slide 21
The gates comes in variety of forms.
  Tab gate
  Fan gate
  Ring gate
  Submarine gate, etc
The gate is always smaller in cross-section than the runner so that the part may detach cleanly and easily.
Because of the small size, gates also impart some shear to the melted plastic as it enters the cavity.
Excessive shear is not desirable and can cause cosmetic and physical imperfections in the part.

## Slide 22
A closer look into Figure 7.4, a feature called a slug well.
Because the initial surge of material will cool as it goes through the sprue and runner, a ”slug” of this cooler material may develop.
The failure to “sidetrack” this slug could cause stresses during injection.
An extension to portions of the runner system, where a corner exists, allows the slug to be “sidetracked” and remain in this slug well.
A large slug well is also designed just below the sprue to accomplish the same purpose.

## Slide 23
The runner systems that have been discussed here are “cold runner systems”, meaning that the runner are not heated.
The outer portion of the melted plastic in the runner system develops a “skin” of semi-solidified melt that insulates the center portion of the melt flow in the runner.
The “hot runner systems” are heated by an external means to keep the plastic in the runner in molten form. Theses system involve a different type of mold design.

## Slide 24: Cold Runner Molds
The runner system is not heated and solidifies in the same manner as the part.
The runner system is then ejected along with the part.
As shown in Figure 7.1, the two-plate mold requires an external force to separate the parts from the runner system. This type of cold runner mold is ideal for parts requiring large gates.
An alternative cold runner mold design is a three-plate mold which allows top center gating and differs from the two-plate mold by the addition of a third plate referred to as a runner plate.

## Slide 25
Figure 7.5 Three-plate mold in a closed position. PL1 is parting line when mold first opens. PL2 and PL3 are second and third parting lines

## Slide 26
Instead of the runner system being located in the “B” plate as shown in Figure 7.1, it is contained in the runner stripper plate, allowing the desired center top fating of the part.
When the mold opens, the part are degated, leaving the runner system the runner system in the runner stripper plate.
Continued movement of the core and cavity halves of the mold, combined with some bolts (tie rods and stripper bolts) that restrict the movement of the runner stripper plate, result in stripping the runner system and sprue off of undercut pins (sucker pins) located in the top clamp plate, allowing the runner system and plastic sprue to fall down out of the mold.

## Slide 27
The three-plate mold is unique in that it opens in three places
  PL1 – Between the runner plate and the stripper plate;
  PL2 – Between the core and the cavity plates;
  PL3 – Between the top clamping plate and the stripper plate.
The mold opens first at P.L.1, breaking the gate and leaving the runner attached to the stripper plate because of the sucker pins.
The mold then opens at P.L.2, leaving the part on the core awaiting ejection.
The final opening at P.L.3 occurs as the mold opens further, stripping the runner off of the sucker pins.

## Slide 28
The three-plate mold in Figure 7.5 is shown with ejector pins.
A mold of this type would frequently utilize a stripper plate rather than ejector pins.

## Slide 29: Hot Runner Molds
The runners are maintained in a heated condition to keep the molten plastic in a fluid state at all times.
Sometimes the hot runner molds are referred to as “runnerless” molds.
Hot-runner molds are similar to three plate molds, except that the runner system is contained in a runner plate that is never opened during the cycle.
This heated runner plate is insulated from the rest of the cooled mold.

## Slide 30
Hot runner molds offer several advantages over cold runner molds.
There is no runner system and sprue molded as a by-product the must be ground up and reused.
Sprue pickers or special conveyors that separate the runner system and sprue from the part are not required.
A uniform melt temp can be maintained all the way from the nozzle to the cavity, insuring fewer deviations in part quality due to a melt that is not isothermal.
The shot capacity and clamp tonnage required in the IMM are decreased.

## Slide 31
Some disadvantages to hot runner molds are
Difficulty in controlling their temp
Inability to purge
Making repair a time consuming process
Not able to change color easily.
Two types of construction for hot runner molds
  Insulated runner molds
  True hot runner molds

## Slide 32
The insulated runner mold has runner that are very thick and are contained partly in the top clamping (or backup plate) and partly in the “A” plate.
The size of the runner allows the development of a thick “skin” of plastic around the outside perimeter of the runners which insulates the molten plastic on the inside of the runner.
These molds are often assisted by heated torpedeos that are inserted in each gate and are kept in a continually heated condition.
When started up, the cold runner system is removed by separating the backup plate from the “A” plate and reassembling them.

## Slide 33
For the true hot runner mold, the runner system is kept not by heating the runner plate itself or by using a heated manifold through which the runner system moves (hot manifold mold).
The distinction of the hot runner mold is the ability to start up cold without intervention by an operator.
As shown in Figure 7.6, the electrically heated manifold and insulated nozzle that are common to this type of mold.
The heated runner system within the manifold is insulated from the rest of the cooled mold.

## Slide 34
The runner section of the mold does not open during the molding cycle.
The parting line of the mold is noted in the figure and the part is held onto the core by undercuts as the mold opens.
As opening, the part is ejected off of the core by ejector pins, a stripper plate or other ejection mechanism.

## Slide 35
Figure 7.6 Hot runner mold in a closed position

## Slide 36: Ejection
The type of ejection discussed in the earlier sections is described as hydraulic ejection.
It offers several advantages;
  It can be actuated at any point in the mold opening stroke;
  It offers the possibility of multiple ejection when operating in the automatic mode to insure complete ejection of the molded parts;
  It allows for the sequencing of core pulls which may require ejection before and after the core pull action;
  The length, velocity and pressure of the ejection stroke can be regulated.

## Slide 37: Assignment
Air cylinder ejection is used to “blow” the part off of the core.
Find more information regarding Air cylinder ejection system. The information should covers;
  Working principle
  Schematic diagram
  Applications (where and why to use this system)

## Slide 38: Projected Area
Is the area in the mold that will be filled with plastic at the mold’s parting line.
The parting line of a mold is the primary opening of the mold where the core and cavity halves separate, allowing the parts to be ejected.
The projected area has also been defined as the area of the shadow cast by the molded shot… on a plane surface parallel to the parting line.
This includes the runner system.
The projected area of the mold is used to establish the tonnage of an IMM that is required to run a particular mold.

## Slide 39: Projected Area
Its important to understand how to calculate the projected area of a mold.
Figure 7.7 Projected area for a four cavity mold

## Slide 40: Projected Area
Assuming;
  Runner system occupies = 4 in2 (2580.64 mm2)
  Each part covers = 24 in2 (15483.84 mm2)
  Thus, total projected area = (4 + 96 = 100) in2 or 64,516 mm2)
In general, every 1 in2 requires 2.5 to 3 tons clamp force.
Accordingly, the projected are of the mold in this illustration should require 250 to 300 tons of clamp force.
Thinner parts typically require greater clamping force that thick-walled parts.

## Slide 41: Projected Area
A higher clamping force is required when;
  Molding with a higher temp. melt
  A hotter mold
  Larger gates
  Faster rate of injection
The steel molds can be crushed by too much clamp pressure.
Some authorities estimate that mold destruction requires only 10 tons/in2.

## Slide 42: Mold Venting
Venting is the method of allowing the air that is trapped inside the cavity space (and the runner system) to escape.
As plastic injected into the closed mold, it traps any air that is in the cavity.
If the air has no place to escape;
  It will be compressed and heated to a temp sufficient to burn the plastic.
  Black and brown spots/streaks in the molded part.
If there is sufficient air trapped in the cavity, the air may prevent the part from being completely filled, causing a rejected part.

## Slide 43: Mold Venting
Venting is accomplished by creating a very small gap or opening at the edges of the cavity.
The opening are small enough (0.00013 to 0.00038 mm) deep and (0.01 to 0.305 mm) long, to allow the air to escape but not the molten plastic.
In addition to vent gaps, there are vent grooves into which the vents exhaust.
The grooves are deeper than the gaps, 0.762 mm deep, and 6.35 to 12.70 mm wide, and must connected to atmosphere to permit release of the trapped air.

## Slide 44
Figure 7.8 Illustration of typical venting of a mold cavity.

## Slide 45: Mold Cooling
The function that is not controlled by the IMM, but rather by an external source.
It accomplished by the proper construction of cooling channels in the mold itself and a Mold Temp. Controller (MTC).
The MTC is connected to the mold water lines and also to either a chiller or water source.
Its controls the temp. and velocity of the water that flows through the mold.
One of considerations in selection of the type of material for a mold is the thermal conductivity (tc).
Tool steel is twice the tc of stainless steel
Beryllium copper is twice the tc of tool steel.

## Slide 46: Mold Cooling
Cooling channels are holes drilled through the cores and cavities and they should be as close as possible to the surface of the plastic.
Typical channel diameter at least 6.35mm and 9.53mm is preferable.
A well designed mold should have several cooling channels that surround the cavities and intrude into the cores to provide uniform and effective cooling.

## Slide 47
Figure 7.9 Illustration of the incorrect looping of mold cooling lines.

## Slide 48: Mold Cooling
Multiple loops off of the same inlet source decrease the cooling effect of the water because of its repeated exposure to warm cavities without a new cool water source.
It is important that temp. of the water coming out of the mold be no more than (2oC) greater than the temp of the water coming in.

## Slide 49
Figure 7.10 Illustration of preferred configuration of mold cooling lines.